## Slide 1: Determination of Thorium and Uranium in Detector material using Inductively Coupled Plasma Mass Spectrometry
Ying YUAN, Hao QIAO, Siguang WANG
School of Physics, Peking University

## Slide 2: Outline
Brief introduction to Trace determination Lab
Experiments
  Stainless Steel
  Copper
  MicroMegas
  3D Printer Raw Material “Feinpolyamide PA 2200 for EOSINT P”
Summary

## Slide 3: Brief introduction to Trace determination Lab

## Slide 4: Cleanliness Measurement in Sample Preparation Room (Apr. 16,2016)

## Slide 5: ICP-MS (Agilent 7900)
The injection port：
Class 10 laminar flowhoods
Isotope dilution analysis using radioactive tracers for U and Th
Notes: 载气将样品气溶胶载到等离子体的中心，进而样品发生干燥、去溶剂、解离、原子化和电离等过程
在管子的上部环绕着一水冷感应线圈，当高频发生器供电时，线圈轴线方向上产生强烈振荡的磁场。用高频火花等方法使中间流动的工作气体电离，产生的离子和电子再与感应线圈所产生的起伏磁场作用，这一相互作用使线圈内的离子和电子沿图市所示的封闭环路流动；它们对这一运动的阻力则导致欧姆加热作用。由于强大的电流产生的高温，使气体加热，从而形成火炬状的等离子体。

## Slide 6: Experiments
Stainless Steel
Ca. 1 g
Surface treatment
Dissolved in aqua regia(王水)
Diluted
Analyze
Detection Limits：
(Blank sample dilution:TDS<0.05%)
0.001 pg 232Th/g (0.05 μBq 232Th/kg)
0.019 pg 238U/g (0.24 μBq 238U/kg)
Preliminary results |  | 
Samples | Th-232 （pg/g)* | U-238 （pg/g)*
P4TC | 378 17 | 312  24
P4TF | 606 129 | 1087 100
P4TN | 30350 | 75571
P4TM | 30976 | 60086
P4TO | 5610 | 1026100
P4TP | 87258 | 76487
*Note：averagestdev
39K in P4TO: 27、26 and 28(ng/g) for 3 samples

## Slide 7: Experiments
Single Crystal Copper
Ca. 0.85 g
flow rate ：0.8 mL/min
Surface treatment
Dissolved in 8 M HNO3 (spiked with 230Th and 235U)
Loaded on the Extraction Chromatography Column
Analyze
Detection Limits：
0.035 pg 232Th/g (0.14 μBq 232Th/kg)
0.073 pg 238U/g (0.90 μBq 238U/kg)
Preliminary results |  | 
Sample | 232Th pg/g | 238U pg/g
Cu 1 | 0.220.07 | 0.370.08
Cu 2 | 0.28 0.14 | 0.370.07
Cu 3 | 0.270.07 | 0.590.19
Cu 4 | 0.160.07 | 0.580.033
Cu 5 | 0.140.07 | 0.540.15

## Slide 8: Experiments
MicroMegas
Surface treatment
Microwave Digestion with concentrated HNO3(spiked with 230Th and 235U)
Loaded on the Extraction Chromatography Column / Diluted
Analyze
Detection Limits：
0.24 pg 232Th/g (0.97 μBq 232Th/kg)
0.14 pg 238U/g (1.73 μBq 238U/kg)
“GEM”
“BIPO”
Preliminary results |  | 
Sample | 232Th pg/g | 238U pg/g
GEM 1 | 36 16 | 2737
GEM 2 | 34 13 | 30842
GEM 3 | 11825 | 29234
BIPO 1 | 46 | 287
BIPO 2 | 43 | 266

## Slide 9: 3D Printer Raw Material
3D Printer Raw Material “Feinpolyamide PA 2200 for EOSINT P”
Over simplified method summary:
Sample into microwave digestion instrument
Dissolve in nitric acids
Dilute and analyze
Sample | Weight g | 232Th pg/g | 238U pg/g
1 | 0.09522 | 283 | 3586
2 | 0.09369 | 290 | 3386
Preliminary results

## Slide 10: Summary
A nice experimental environment for trace determination have been established. Cleanliness can be ISO Clean 10.
The analysis method for determining Th and U content in copper, stainless steel, micromegas was established.
The condition for 3D Printer Raw Material is being optimized.
Method Detection Limits (preliminary results) |  | 
Sample | MDLs 232Th pg/g | MDLs 238U pg/g
Copper | 0.035 | 0.073
Stainless Steel | 0.001 | 0.019
MicroMegas | 0.24 | 0.14

## Slide 11
Thanks！